## Slide 1: Exciting the spin transitions of with Propagating Microwaves via Superconducting Electrical Circuits
Hayden Nathanael Tanis
Technische Universität München
Walther-Meissner Institute

## Slide 2: Introduction

## Slide 3: Chapter 2: Rare-Earth Physics and Spin Dynamics

## Slide 4: Rare Earth Elements

## Slide 5: Host Material
Figure: Unit Crystal of Calcium Tungstate

## Slide 6: Erbium Dopants in Calcium Tungstate
Total Hamiltonian consists of the free-ion energy, crystal field term, and the spin-Hamiltonian.

## Slide 7: Erbium Dopants in Calcium Tungstate
1. Free Ion
  Affected by kinetic energy, potential energy, Coulomb potential, spin-orbit coupling
  Russel-Saunders notation of the ground state and the first excited state of free erbium ions:
  Ground state:
  First Excited state:

## Slide 8: Erbium Dopants in Calcium Tungstate
2. Crystal Field
  Embedding erbium ions within a crystal will break the local symmetry of the electronic structure
  The ground state will split into 8 doubly degenerate Kramer’s doublets, denoted:
  In sub-Kelvin temperatures, only the lowest Kramer’s doublet is populated

## Slide 9: Erbium Dopants in Calcium Tungstate
3. Spin Hamiltonian
  The effective spin-Hamiltonian of Erbium consists of the following terms:
    Electron-Zeeman Interaction
    Hyperfine Interaction
    Nuclear Quadrupole Interaction

## Slide 10: Erbium Dopants in Calcium Tungstate
Known spin-Hamiltonian parameters of Erbium isotopes

## Slide 11: Erbium Dopants in Calcium Tungstate
Energy Structure of Erbium

## Slide 12: Spin Dynamics
Two-level quantum systems
The quantum state of any arbitrary two-level quantum system can be represented as a superposition of the ground state and the excited state.
Standard representation of a two-level quantum system via Bloch Sphere
A Kramer’s doublet can be treated as an effective spin S = ½ system which is a two-level quantum system

## Slide 13: Spin Relaxation Mechanisms
Relaxation Processes
Energy exchange with a bath when out of thermal equilibrium
Two Relaxation Rates in the Bloch-Redfield model
  Spin-Lattice Relaxation (also known as Longitudinal relaxation)
  Spin-Spin Relaxation (also known as Transverse Relaxation)

## Slide 14: Spin Relaxation Mechanisms
Spin-Lattice Relaxation (SLR)
Rate with which an electron spin returns to thermal equilibrium
Interaction between spins and crystal lattice will induce energy loss
In the Bloch Sphere: The longitudinal component of the state vector will return to its ground state after a period of time (T1 time)
In complex systems with multiple energy levels - decay to thermal equilibrium will follow a multi-exponential decay function

## Slide 15: Spin Relaxation Mechanisms
Processes behind Spin-Lattice Relaxation (SLR)
Main processes
Process | Direct Phonon Process | Raman Process | Orbach Process
Type | Single phonon process | Higher order process (two phonon interaction) | 
Contribution in sub-Kelvin temperature | Direct exchange of phonons between crystal lattice and spin-system Main process governing SLR in sub-kelvin temperatures | Effect is negligible at sub-kelvin temperatures. | 

## Slide 16: Spin Relaxation Mechanisms
Spin flip-flop interactions
Caused by the interaction between the magnetic dipoles of two spins – induces cross relaxation if the two spins are spatially close to each other
Flip-flop interaction dominates the relaxation rate at low magnetic fields
At higher fields, the direct phonon process will overpower the flip-flop interaction

## Slide 17: Chapter 3 Experimental Methodology

## Slide 18: BEPR with Superconducting Coplanar Waveguides

## Slide 19: Measurement Setup

## Slide 20: Power Sweep
Higher VNA power, shallower absorption dip
Maximum VNA power for probing: -42 dB

## Slide 21: Saturation Recovery Measurements

## Slide 22: Chapter 4 Results and Discussion

## Slide 23: Zero-Field Spectroscopy
Spectroscopy measurements done in zero-magnetic field
Identifies hyperfine transitions
  Energy level splitting determined by field independent terms
  Zeeman interaction does not play a role
Following measurements
  Broadband ZF-Spectroscopy of the sample
  Narrowband Spectroscopy show detected spin transitions
Notes: Firstly I would like to present the results of spectroscopy measurements done under zero magnetic field conditions.

## Slide 24: Zero-Field Spectroscopy
Broadband Spectroscopy
Notes: Firstly I would like to present the results of spectroscopy measurements done under zero magnetic field conditions.

## Slide 25: Zero-Field Spectroscopy
Hyperfine Transitions
2.7 GHz transition
2.6 GHz transition

## Slide 26: Zero-Field Spectroscopy
Hyperfine Transitions
3.2 GHz transition
3.4 GHz transition

## Slide 27: Magnetic Field Sweeps

## Slide 28: Magnetic Field Sweeps
Offset ca. 0.2mT

## Slide 29: Circle Correction Procedure
Original datasets in complex plane

## Slide 30: Circle Correction Procedure
Corrected datasets

## Slide 31: Circle Correction Procedure
Original vs Corrected Dataset in S21 vs Frequency plane

## Slide 32: Field Dependent Measurements
Aim: observe how T1 relaxation time changes under the influence of low magnetic fields
Focus: Characterization of the 2.6 GHz spin transition in the presence of different magnetic fields
Magnetic Field (mT) | 0.3 | 0.55 | 0.8 | 1.05 | 1.3
VNA Center Frequency (GHz) | 2.65406 | 2.65362 | 2.6526 | 2.6513 | 2.6495

## Slide 33: Magnetic Field Sweeps

## Slide 34: Chapter 5 Conclusion